PRODUCT DATA

FRS-108 Polyurethane sealant

1 、Product Description：

This product is a one-component polyurethane sealant with the characteristics of high strength, good adhesion, low odor, low volatility, and non-corrosiveness. It has heat resistance and good adhesion to glass, metal and other substrates.

2 、Typical uses：

① Used for bonding front and rear windshields, side windows and car bodies. It is widely used in automobiles, special vehicles, train carriages, ships, etc.

② Used for sealing of passenger car floors and sheet metal seams, sealing of weld seams in refrigerated carriages, containers, etc., and bonding and sealing of window glass in the maintenance market.

3 Performance parameters before curing：

| Chemical type | polyurethane |
| --- | --- |
| Color | white/black/grey/customized |
| Density | 1.43±0.05g/cm³ |
| Surface drying time | ≈60minutes |

4 、Performance parameters after curing：

| Tensile strength（MPa） | 4 |
| --- | --- |
| Sealing time | 即时密封 |
| Shear strength（MPa) | 2 |
| Hardness (Shore) | 15~25 |
| Elongation at break | 400% |
| Heat resistance | Good |

5、Curing properties：

FRS-108 is mainly cured by reacting with moisture in the atmosphere. It cures in place at room temperature. It is easy to use and non-corrosive to metals.

6、How to use：

①Clean the construction surface to ensure it is dry and free of oil and dust;

② Paste protective tape on both sides of the construction. If the joint is too wide, fill the joint with lining material;

③Remove the metal sealing aluminum foil at the rear end of the aluminum tube, cut the bottle mouth, install the glue nozzle, cut the glue nozzle according to the required size, and extrude it with a glue gun;

④ The sealant squeezing action should be carried out continuously to make the glue evenly squeezed out and move evenly and slowly to ensure that the joint is filled with sealant. It is necessary to prevent the nozzle from moving too fast and causing bubbles or cavities;

⑤ Complete the trimming within 10 minutes after gluing and remove the protective tape.

7 、Things to note：

①After gluing, do not touch the sealant before the surface is dry to avoid damaging the surface smoothness of the sealant;

②Before the sealant is cured, ensure that the surrounding environment is ventilated and dry;

③Please place it in a place out of reach of children;

④ Please use it as soon as possible after opening;

⑤Not suitable for loose surfaces;

⑥Do not let uncured products come into contact with your eyes. If it accidentally gets into your eyes, please wash it with clean water and seek medical treatment promptly.

8、illustrate：

The various data contained herein are provided for informational purposes only and are believed to be reliable. Our company is not responsible for the results obtained by anyone using methods beyond our control. It is the user's own responsibility to decide which production method to use this product on and which measures to take to prevent possible losses and personal injuries during storage and use of the product. If you have any questions, please contact the company's technical department.

E-mail: lihaoran6789@126.com

Shandong Furuisi New Material Technology Co., Ltd.